APTES and DSC-FUNCTIONALIZED COVERSLIPS

Materials

Sulfuric Acid (H2SO4)				3-Aminopropyltriethoxysilane (Sigma)

Hydrogen Peroxide (H2O2)				Coverslips

H2O							EtOH

Disuccinimydil carbonate	ECM protein or peptide of interest (must contain functional amine)

1M Tris buffer					PBS

Methods

aptes-functionalization

- Treat coverslips with Piranha (25% H2SO4, 15% H2O2) for 1 hour on an orbital shaker.  Piranha is highly toxic!  Make solution in the hood and make sure to dispose of it safely.

- Sonicate coverslips while in piranha for 15min.

- Rinse coverslips thoroughly with H2O and EtOH.

- Add 10mL of APTES in 200mL of 95% EtOH to coverslips and incubate on shaker for 1 hour.

- Wash coverslips thoroughly with EtOH and H2O.

- Dry coverslips under Nitrogen.

- Heat coverslips to 110oC for 20min in glass drying oven.

DSC-functionalization

- Add 1.5g of disuccinimydil carbonate (DSC), 5mL of DIEA, in 145mL of dry acetone to coverslips, incubate for 2 hours on shaker.

- Wash coverslips thoroughly with dry acetone.

- Dry coverslips completely under Nitrogen.

- Store coverslips in dessicator.

protein coupling

- Attach desired ECM proteins or short peptides to coverslips by diluting proteins in PBS to desired concentration.

- For an 18mm coverslip, pipette 100uL of protein solution onto a parafilm surface, and cover solution with DSC-coupled coverslip.

- Allow to react for 4 hours.

- Post-reaction, wash coverslips thoroughly with PBS.

- Block coverslips with 1M Tris buffer for 1 hour.

- Wash coverslips thoroughly with PBS.

- Sterlize coverslips via UV-light irradiation for at least 20min prior to cell seeding.